|  |  | Compressive Strength of Cement Stabilized Soils. A New Statistical Model Dr. Costas A. Anagnostopoulos Laboratory of Soil Mechanics and Foundations, Geotechnical Engineering Division, Department of Civil Engineering, Aristotle University of Thessaloniki, 541 24 Thessaloniki Greece, Tel: 0030 2310 995706 kanagnos@civil.auth.gr Dr. Maria Chatziangelou Laboratory of Engineering Geology and Hydrogeology School of Geology Aristotle University of Thessaloniki 540 06 Thessaloniki, Greece, Tel: 0030 2310 998506 mcha@geo.auth.gr |
| --- | --- | --- |

ABSTRACT

Soft soils are well known for their low strength properties, high compressibility and high swell-shrinkage characteristics. Thus, they are inappropriate for building foundation or for other geotechnical works. Deep cement mixing has recently been used to face these problems by improving the strength and reducing the deformation of soft soils. The present study examines the parameters which influence significantly the strength of a cement stabilized soil. These are: the water and sand content, the liquid limit, the amount of the added cement and curing time. A comprehensive laboratory work was carried out in order to study the compressive strength of nine different silty-clay soils stabilized with various quantities of cement. The laboratory results were used for the development of a non linear regression equation that best relates the compressive strength of a stabilized soil to the aforementioned parameters considered as descriptor variables.

KEYWORDS: Soil stabilization, compressive strength, regression model

INTRODUCTION

The Deep Mixing Method (DMM) is today accepted world-wide as a soil improvement method which is performed to improve the strength, deformation properties and permeability of the soil. It is based on mixing binders, such as cement, lime, fly ash and other additives, with the soil by the use of rotating mixing tools in order to form columns of a hardening material since pozzolanic reactions between the binder and the soil grains are developed. The most common binder that is used in DMM, because of its appreciable effect on improving the soil properties, is cement.

This method is often applied on many geotechnical and foundation applications such as the stabilization of deep excavations or high embankments, the reduction of settlement or the increase of soil strength for building foundation, the slope stability, the tunnel support, the water retention etc. The strength of soil-cement mixture (the most common binder that is used in DMM) is influenced from many parameters like physicochemical properties of the soil, geological and hydrogeological conditions of the area, the properties and the quality of the used binder or the additive, the mixing method and consequently the mechanical equipment, the curing conditions (Porbaha, 2000). Because of the aforementioned parameters, a significant deviation between the laboratory measurements of strength of soil-cement specimens and the corresponding one taken from in situ is usually observed.

A significant research has been done from Omine and Ohno (1997) concerning the estimation of the in situ compressive strength based on laboratory measurements of compressive strength and other parameters obtained from the construction phase of soil-cement column. The model which is suggested has a good approach. Consequently, the measurement of the strength of soil-cement mixtures in laboratory and the determination of the parameters which affect it is still very important for the estimation of strength of mixture in situ (Porbaha, 2002).

The objective of the present paper is to develop a new model, based on regression analysis, for predicting the compressive strength of a cement stabilized soil under laboratory conditions from parameters such as liquid limit (wL)of the soil, water content (w), percentage of the added cement, sand content and curing time which strongly affect its value. The quality of cement was not taken into account on the proposed model, since previous studies has shown that it has a limited influence on the strength of the stabilized soil (Ahnberg et al., 2003).

Materials used-laboratory procedure

The soil type can affect significantly the efficacy of cement stabilization (Puppala et al., 2003). For this reason, nine types of soils were stabilized with different quantities of cement in order to obtain a large variation of compressive strength values. Seven of the soils were inorganic clays of high plasticity (CH) with some of them containing considerable amount of (SO4)-2, one soil was inorganic clay of medium plasticity (CI) and one soil was organic clay of high plasticity (OH) containing 10% of organic material. Table 1 represents the basic geotechnical properties of the used soils. Portland cement with blaine fineness of 4,500cm2/g, specific mass of 3.15g/cm3 and 28-day compressive strength of 45 MPa, was used for stabilization experiments. Soils were treated with cement dosages ranging from 5 to 30% by dry unit weight of soil. Cement-soil specimens tested in unconfined compression were prepared by initially mixing the relevant quantities of dry soil and water for at least 5 minutes with a high rotating stirrer; the cement was then added to the mixture and further mixing was performed until it was homogeneous in appearance. Cylindrical specimens were prepared by pouring the soil-cement material into moulds, 35.5mm in diameter and 71mm height (ASTM, 1996). Compressive strength tests were performed under a constant strain rate of 0.6604 mm/min. Table 2 shows the curing time of soil-cement mixture specimens and the percentage of water-cement addition.

Results and discussion

Figures 1(a)-(c) present the compressive strength values of different soils stabilized with cement dosages ranging from 5 to 30% by dry weight of soil at 7, 28 and 90 days of curing. A significant variation of strength values for all ages  of curing and for all cement dosages is

Table 1. Basic properties of the tested soils

| Properties | S1 | S2 | S3 | S4 | S5 | S6 | S7 | S8 | S9 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth (m) | 10-12 | 10-15 | 3-6 | 2-5 | 3-5 | 10-15 | 15-20 | 10-15 | 10-15 |
| Density (t/m3) | 1.592 | 1.668 | 1.55 | 1.52 | 1.23 | 1.62 | 1.596 | 1.644 | 1.67 |
| Unit weight of solids (t/m3) | 2.67 | 2.7 | 2.72 | 2.73 | 2.36 | 2.87 | 2.8 | 2.76 | 2.85 |
| Liquid limit (%) | 87 | 43.54 | 70 | 66 | 170 | 69.4 | 69 | 70.6 | 73.96 |
| Plastic limit (%) | 35 | 25.32 | 24 | 23 | 64 | 26.7 | 27.9 | 28.4 | 28.92 |
| Plasticity Index (%) | 52 | 18.22 | 46 | 43 | 106 | 42.7 | 41.1 | 42.2 | 45.04 |
| Silt-clay content(%) | 90 | 67 | 63 | 72 | 80 | 90 | 93 | 89 | 91 |
| Sand content(%) | 10 | 33 | 37 | 28 | 20 | 10 | 7 | 11 | 9 |
| Soil characterization | CH | CI | CH | CH | OH | CH | CH | CH | CH |
| Ph | 8.7 | 8 | 7.6 | 8.7 | 8.5 | 7.96 | 8.2 | 8.13 | 8.08 |
| SO4-2 (%) | 0.17 | 0.07 | 0.05 | 0.18 | 0.2 | 0.06 | 0.11 | 0.1 | 0.1 |

Table 2. Curing time of specimens and the percentage of water-cement addition

| Soil | Water addition (% by weight of dry soil) | Cement addition (% by weight of dry soil) | Curing time (days) |
| --- | --- | --- | --- |
| S1 | 110 137 | 5 10 20 30 | 7 28 90 |
| S2 | 60 | 5 10 20 30 | 7 28 90 |
| S3 | 78 | 6,5 | 7 28 90 |
| S4 | 89 | 6,5 | 7 28 90 |
| S5 | 220 | 8,5 | 7 28 90 |
| S6 | 25,3 | 5 10 | 7 28 90 |
| S7 | 27 | 5 10 | 7 28 90 |
| S8 | 27,5 | 5 10 | 7 28 90 |
| S9 | 26 | 5 10 | 7 28 90 |

(a)

(b)

(c)

Figure 1. Variation of compressive strength of soil specimens stabilized with different amounts of cement: (a) 7 days; (b) 28 days and (c) 90 days.

(a)

(b)

(c)

Figure 2. Compressive strength of soil specimens stabilized with 5 and 10% cement in relation to the consistency index: (a) 7 days; (b) 28 days and (c) 90 days.

observed. This fact reflects the substantial influence of the soil chemical composition and the water content over the development and progress of pozzolanic reactions and consequently over the early and final strength of the soil-cement mixture. For example, addition of 10% cement in different soils had as a result strength values ranging from 80 to 2110 kPa at 7 days of curing, 102 to 2600 kPa at 28 days of curing and 131 to 2990 kPa at 90 days of curing. Soils with high liquid limit or high water content exhibited the lowest strength at all ages even though a large amount of cement was added. This is attributed to the intense hydrophilic behavior of soils which is characterized from high liquid limit values. These soils attract and retain high amount of water limiting to some extent pozzolanic reactions and consequently the adhesion between the soil grains and cement crystals affecting adversely the development of strength. Also, the occurrence of large amount of water, leads to the creation of a weak structure between the formed cement crystals and the soil particles. The influence of wL and w on strength is shown in figures 2(a)-(c) at which the compressive strength of soil-cement specimens containing 5% and 10% cement is correlated with the consistency index Ic. The graphical plots visibly indicate the wide variation of compressive strength values at all ages of curing, despite the specimens were stabilized with the same cement dosage. Indicatively reported, addition of 5% cement resulted in 7, 28 and 90 day strength values ranging from 45 to 1040 kPa, 52 to 1196 kPa and 62 to 1690 kPa, correspondingly.

Regression models

Based on the laboratory results and using SPSS 14.0 statistic program a non linear regression model was developed which correlates the compressive strength q of cement stabilized soil to the five variables (water content w (%), liquid limit wL (%), cement content C (%), sand content S (%) and curing time CT (days)) as follows:

q = -326.77 – 1170.09 ln(w) + 1292.06 ln(wL) + 0.523 (C) (S)1.417 (ln(CT))0.608                     (1)

The reliability and accuracy of the model were checked by comparing the predicted values of compressive strength from this model and the measured values, and computing the correlation

Figure 3. Cross plot of measured compressive strength vs. computed values using equation 1.

(a)

(b)

(c)

Figure 4. Cross plot of measured compressive strength vs. computed values.

(a) 7 days (eq. 3); (b) 28 days (eq. 4) nad (c) 90 days (eq. 5).

coefficient. Figure 3 illustrates a plot of the measured values of compressive strength versus the computed values using the non linear regression model. The straight line in the figure represents the line of perfect equality, where the values being compared are exactly equal. The correlation coefficient R2 at 95% confidence interval is 0.877, meaning roughly that 87.7% of the variance in compressive strength is explained by the model. This value is statistically significant and therefore suggests that the measured and calculated values of compressive strength are comparable.

In order to obtain a more accurate regression model the curing time was left out as a descriptor variable in the regression equation. The model that gives the best correlation is of the following form again:

q = a0 + a1 ln(w) + a2 ln(wL) + a3 (C) (S)a4					             (2)

The resulting regression equations that best relates the compressive strength to the four structural descriptors of the soil properties are given:

For 7 days of curing:

q = -316.79 – 1015.82 ln(w) + 1116.03 ln(wL) + 0.964 (C) (S)1.359

R2 = 0.845   				    						 (3)

For 28 days of curing:

q = -308.32 – 1152.96 ln(w) + 1268.29 ln(wL) + 0.958 (C) (S)1.464

R2 = 0.902   				    						 (4)

For 90 days of curing:

q = -560.71 – 1329.13 ln(w) + 1538.22 ln(wL) + 0.808 (C) (S)1.543

R2 = 0.8915 				    						 (5)

The predictive model of 7 day strength has correlation coefficient (R2 = 0.845) slightly lower than the one of the initial model utilized the curing time. On the contrary, the models of 28 and 90 day strength appeared to have correlation coefficients slightly higher. Figures 4(a)-(c) depict the correlation between the measured and the calculated values of compressive strength obtained from the application of equations 3-5.

Conclusions

Both laboratory and field procedures employed in the determination of compressive strength of soil-cement column material are time consuming and expensive. An alternative to the experimental approach is the prediction of compressive strength from parameters easily recorded and measured. The present study used laboratory results in order to obtain a model that best relates the strength to the above aforementioned parameters. Two general models were developed. The first relates the strength to the five structural descriptors whereas the second model does not include the curing time as a variable. Both models show high values of R2 and the comparative assessment indicates that the developed models provide a very good agreement with the measurements.

REFERENCES

- Ahnberg, H., Johansson, S.E., Pihl, H. and Carlsson, T. (2003) “Stabilising effects of different binders in some Swedish soils”. Ground Improvement, Vol. 7, pp 9-23.

- ASTM D1632-96, “Standard Practice for Making and Curing Soil-Cement Compression and Flexure Tests Specimens in the Laboratory”. American Society for Testing and Materials, West Conshohochen, PA.

- Omine. K. and Ohno, S. (1997) “Deformation analysis of composite ground by homogenization method”. Proc. 14th Intern. Conf. on Soil Mechanics and Foundation Engineering, Hamburg, pp 719-722.

- Porbaha, A. (2000) “State-of-the-art in deep mixing technology: design considerations”. Ground Improvement, Vol. 4, pp111-125.

- Porbaha, A. (2002) “State of the art in quality assessment of deep mixing technology”. Ground Improvement, Vol. 6, pp 95-120.

- Puppala, A.J., Wattanasanticharoen, E. and Punthutaecha, K. (2003) “Experimental evaluations of stabilisation methods for sulphate-rich expansive soils”. Ground Improvement, Vol. 7, pp 25-35.